SPECIFICATION FOR FIL.004.13

Drawing ref :- TAV.1440

FLOW RATE 	:-  300 – 900 m3/hr (176 – 530 cfm)

PRESSURE		:- 5 bar (absolute)

TEMPERATURE	:- -40˚C to 150˚C Continuous

ELEMENT		:- Pleated construction .

Outer mesh		:- 40`s square mesh 316 stainless steel

Inner mesh		:- 80`s square mesh 316 stainless  steel

Filter media		:- 5 micron absolute( 98% 1 µ )

316 stainless steel (sintered fibre.)

ASSEMBLY		:- Welded seam. Epoxy bonded end caps.

TESTING	:- Integrity test by bubble point .

ISO	:- All elements carry works order production number .

Unique to each element